## Slide 1
When and How Fracture Nucleates and Propagates in Rubber
Work supported by the National Science Foundation (DMS, CMMI)
April 28, 2020
Center for Nonlinear Analysis, Carnegie Mellon University
Oscar Lopez-Pamies
Collaborators: Aditya Kumar, Gilles A. Francfort

## Slide 2
When and how rubber bands fracture?
Stephen Perry (1845)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 3
When and how rubber fractures?
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 4
When and how brittle materials fracture?
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 5
Brittle fracture
The idea: Griffith (1921)
The mathematical formulation: Francfort and Marigo (1998)
Its phase-field regularization: Bourdin, Francfort, Marigo (2000, 2008)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 6
The phase-field approach to brittle fracture
where are monotonic functions such that
with
Fracture propagation?
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 7
The phase-field approach to brittle fracture
where are monotonic functions such that
with
Fracture propagation
Comparisons with experiments over the last 20 years confirm so
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 8
The phase-field approach to brittle fracture
where are monotonic functions such that
with
Fracture propagation
Fracture nucleation?
Over the last 10 years significant efforts have been devoted to trying to establish that the phase-field formulation is also able to describe fracture nucleation…
Comparisons with experiments over the last 20 years confirm so
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 9
The phase-field approach to brittle fracture
where are monotonic functions such that
with
Fracture propagation
Fracture nucleation
The phase-field approach to brittle fracture
is fundamentally incomplete to describe fracture nucleation
Comparisons with experiments over the last 20 years confirm so
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 10
The basic ingredients for the modeling of fracture nucleation
large pre-existing crack
(crack singularity)
bulk (no singularity)
smooth boundary point
(no singularity)
sharp corner
(weak singularity)
rounded corner
(no singularity)
small pre-existing crack
(crack singularity)
Nucleation in the bulk: the strength
Nucleation from large pre-existing cracks: the critical energy release
Nucleation from the boundary and small pre-existing cracks: the transition zone
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 11
Nucleation in the bulk: the strength
General affine stress BCs
Strength surface
uniform stress
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 12
Nucleation in the bulk: the strength
General affine stress BCs
Isotropic strength surface
Stress invariants
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 13
Nucleation in the bulk: the strength
General affine stress BCs
DP Strength Surface for Titania ( , )
Isotropic strength surface
An example: Drucker-Prager strength surface
Drucker and Prager (1952); Ely (1972)
-1500
-500
500
0
-1500
-500
500
0
-1500
-500
500
0
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 14
Nucleation in the bulk: the strength
Experiments (titania)
DP Strength Surface
General affine stress BCs
Strength Surface for Titania ( )
Isotropic strength surface
An example: Drucker-Prager strength surface
Drucker and Prager (1952); Ely (1972)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 15
Nucleation from large pre-existing cracks: the critical energy release
large pre-existing crack
Critical energy release rate
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 16
Nucleation form the boundary & small pre-existing cracks: the transition zone
Transition zone for Alumina
Kimoto et al. (1985)
small pre-existing crack
(crack singularity)
Transition zone: mediation between the strength and the critical energy release rate
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 17
In summary
Material Input Data:
stored-energy function
strength surface
critical energy release rate
The phase-field approach
is purely energetic and does not account for the strength of the material, which is not an energetic quantity, but rather a stress-based one
This is the reason why the stresses predicted by the phase-field framework for fracture nucleation in the bulk, from the boundary, and from small-cracks become unbounded in the limit as
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 18
Illustration of the purely energetic character of the phase-field framework
For the case when
The strength surface predicted by the phase-field model is given by
0
0
0
2
2
2
-2
-2
-2
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 19
Illustration of the purely energetic character of the phase-field framework
For the case when
The strength surface predicted by the phase-field model is given by
0
0
0
2
2
2
-2
-2
-2
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 20
Illustration of the purely energetic character of the phase-field framework
For the case when
The strength surface predicted by the phase-field model is given by
0
0
0
2
2
2
-2
-2
-2
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 21
Illustration of the purely energetic character of the phase-field framework
Experiments (titania)
P-F Strength Surface
For the case when
The strength surface predicted by the phase-field model is given by
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 22
A new phase-field framework that can describe nucleation
The two-pronged idea is:
To consider the Euler-Lagrange equations of the classical phase-field as the primal model, and
To add an external driving force ce in the Euler-Lagrange equation governing the evolution of the phase field v that brings into the model direct dependence on the strength of the material
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 23
The framework as an Allen–Cahn phase-transition model
Balance principles
Balance of Linear Momentum
Balance of Configurational Forces
Constitutive relations
Stress: conjugate to the strain
Configurational internal force: conjugate to the phase field
Configurational stress: conjugate to the gradient of the phase field
Configurational external force
Gurtin (1996)
Kumar, Ravi-Chandar, Lopez-Pamies Int. J. Frac. (2018)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 24
An example
Material Input:
with
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 25
Nucleation in the bulk: graphite tubes
30
20
90
PA
PA
pi
Sato et al. (1987)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 26
Nucleation in the bulk: polyurethane
Cristiano et al. (2010)
10
1
P,u
R = 18.2
+
1.7
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 27
Nucleation from large pre-existing cracks: PMMA
63.5
15.8
22.86
13.47
60.96
21.48
12.7
16.51
12.7
10
P,u
P,u
x
y
Pham et al. (2017)
front of the pre-existing crack
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 28
Nucleation from a boundary point: the L-shape concrete experiment
250
250
250
250
30
P,u
Experiment
(front side)
Experiment
(back side)
Phase-field
Winkler (2001)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 29
Nucleation from a small pre-existing crack: alumina
s
s
40
6
a
Kimoto et al. (1985)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 30
Going finite deformations: a few more historical notes on rubber
Vulcanization of natural rubber
Charles Goodyear (1844)
The fracture mechanics of rubber
Nucleation in the bulk (a.k.a. cavitation)
Nucleation/Propagation from a large pre-existing crack
Busse (1934)
Gent and Lindley (1959)
Rivlin and Thomas (1953)
Griffith (1921)

## Slide 31
The actual story as revealed by new high-resolution experiments
glass spheres
Rate of macroscopic loading
Spatiotemporal resolution
Geometry
transparent PDMS 45:1 matrix
  Poulain, Lefèvre, Lopez-Pamies, Ravi-Chandar Int. J. Frac. (2016)
  Gent and Park (1984)

## Slide 32
The actual story as revealed by new high-resolution experiments
glass spheres
Rate of macroscopic loading
Spatiotemporal resolution
Geometry
transparent PDMS 45:1 matrix
  Poulain, Lefèvre, Lopez-Pamies, Ravi-Chandar Int. J. Frac. (2016)
  Gent and Park (1984)

## Slide 33
The actual story as revealed by new high-resolution experiments
unloaded

## Slide 34
Some key remarks
Remark III: The nucleation of “cavities” is fundamentally a by-product of fracture and not solely of elasticity
Remark II: The nucleation of “cavities” is an extremely fast process involving stretch rates in excess of 100 s-1
Remark I: The nucleation of “cavities” is stochastic in nature
10 mm diameter
“cavity”
10 mm diameter “cavity”
d diameter
submicron defect
Remark IV: The “cavities” are actually deformed cracks
initial penny-shaped
crack (150 mm diameter)

## Slide 35
The phase-field model in finite deformations
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 36
An example
Material Input:
and
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 37
Calibration of PDMS 30:1
Lopez-Pamies C R Mecanique (2010)

## Slide 38
s1 (MPa)
s2 (MPa)
s3 = s2
s1 (MPa)
s2 (MPa)
s3 (MPa)
-2
0
-2
0
1
0
-2
1
1
-1
-1
-1
Calibration of PDMS 30:1

## Slide 39
Some Validation: Fracture nucleation within the bulk of PDMS 30:1
PDMS 30:1,
1st cycle
Kumar, Ravi-Chandar, Lopez-Pamies Int. J. Frac. (2018)

## Slide 40
Back to when and how rubber bands break
d0
d0
e3
e1
l0 = 20×d0 = 40 mm
l0 = d0/13.3 = 0.15 mm
l0 = d0/35 = 0.057 mm
d0
u, P
d0 = 2 mm
e1
e3
e1
e2
l0
very short band
short band
long band
Stephen Perry (1845)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 41
When and how rubber bands break
The poker-chip experiment Gent and Lindley (1959)
The “simple” tension experiment
Smith (1964)
very short band
short band
long band
elastomer
midplane
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 42
Very short band
l
s (MPa)
l = 1.028
l = 1.067
l = 1.150
e1
e2
e1
e2
l = 1.150
e1
e2
e1
e2
e1
e2
e3
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 43
Short band
l = 1.105
l = 1.120
l = 1.150
e1
e2
e1
e2
e1
e2
l = 1.150
e1
e2
e3
l
s (MPa)
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 44
Long band
l
s (MPa)
l = 4.01
e3
e1
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 45
Warning on surface defects
15 mm
5 mm
a
u, P
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.

## Slide 46
Three take-home messages
Basic Ingredients:
stored-energy function
strength surface
critical energy release rate
A Promising Approach:
Many mathematical questions remain open!
Notes: The theory is predicated on two basic ideas.
So consider these solid that has two phases. Z=1: solid phase and z=0 the fractured phase.